The Effects of Primers on the Shear Bond Strength of Orthodontic Metal Bracket to Zirconia Restorations

Seo-Hyun Lee

Department of Dental Science

Graduate School, Chonnam National University

(Supervised by Professor Jin-Hyoung Cho)

(Abstract)

This study was conducted to investigate the effect of primers on the shear bond strength of orthodontic metal brackets to varied types of zirconia restorations. Three types of zirconia based ceramics were used in this study: naked zirconia, glazed zirconia, and porcelain veneered zirconia. Total 240 specimens were prepared and sandblasted at constant pressure and distance, and then pretreated with zirconia primer        (Z-PrimeTM Plus), multi-use primer (Assure® Plus) and silane primer (Porcelain Conditioner) for each 80 specimens, respectively. Two brackets were bonded using two adhesive resins, TransbondTM XT and Light   Bond™. Non-thermocycling group was stored in distilled water at 37℃ for 24 hours and thermocycling group was thermocylced for 3000 cycles. Shear bond strength was measured and the results were obtained as follows.

1. In non-thermocycling group, all groups showed clinically applicable shear bond strength except naked zirconia in Porcelain Conditioner group.

2. Thermocycling group showed statistically significant lower shear bond strength compared to non-thermocycling group. However, application of Z-PrimeTM Plus and Assure® Plus for naked zirconia, Assure® Plus and Porcelain Conditioner for glazed zirconia, and Porcelain Conditioner for porcelain veneered zirconia showed statistically significant higher values for clinical use.

These results indicate that the use of appropriate primers should be considered depending on the type of zirconia restorations.

지르코니아 수복물과 교정용 브라켓 간의 전단결합강도에 대한 프라이머의 효과

이 서 현

전남대학교 대학원 치의학과

(지도교수 : 조진형)

(국문초록)

본 연구는 다양한 지르코니아 수복물에 교정용 브라켓을 접착할 때 사용되는 프라이머가 브라켓의 전단결합강도에 미치는 영향을 알아보고자 시행되었다. 임상에서 사용되는 지르코니아 수복물을 순수 지르코니아, 글레이징 처리된 지르코니아, 도재 소성 지르코니아 등 세 가지 종류로 구분하여 각각의 지르코니아 수복물을 재현한 시편을 종류별로 80개씩 240개를 제작하였다. 이를 일정한 압력과 거리에서 샌드블라스팅한 후 지르코니아 전용 프라이머(Z-PrimeTM Plus), 다목적용 프라이머(AssureⓇ Plus), 도재 전용 프라이머(Porcelain Conditioner)를 이용하여 각각 전처리를 하였으며, 프라이머 전처리 없는 군은 대조군으로 사용하였다. 브라켓은 두 종류의 접착 레진(TransbondTM XT, Light BondTM)을 사용하여 제조사의 지시에 따라 접착하였다. 37℃의 증류수에 24시간 보관한 후 전단결합강도를 측정한 군과 3000사이클의 열-순환 처리를 시행한 후 전단결합강도를 측정한 군을 분석하여 다음과 같은 결과를 얻었다.

1. 열-순환 처리를 시행하지 않은 경우 순수 지르코니아에서 Porcelain Condi- tioner를 사용한 군을 제외한 모든 군에서 임상적으로 사용 가능한 전단결합강도를 보였다.

2. 열-순환 처리를 시행한 경우에는 전반적으로 낮은 전단결합강도를 나타내었으나 순수 지르코니아에서는 Z-PrimeTM Plus와 AssureⓇ Plus, 글레이징 처리된 지르코니아에서는 AssureⓇ Plus와 Porcelain Conditioner 그리고 도재 소성된 지르코니아에서는 Porcelain Conditioner를 처리한 군에서 통계적으로 유의하게 높은 값을 보였으며, 이는 임상적 사용에 충분한 전단결합강도를 나타내었다.

이상의 연구 결과는 지르코니아 수복물의 종류에 따른 적절한 프라이머의 사용에 대한 고려가 필요함을 나타내었다.