전해연마후 교정선의 변화에 관한 실험적 연구

이  재  철

전남대학교 대학원 치의학과

(지도교수 : 김  종  철)

(초록)

교정용호선을 따라서 치아가 움직일 때 교정용호선, bracket 그리고 결찰재 사이에서 마찰력이 발생하게 되는데, 교정적 치아 이동시 이러한 마찰력은 제거되거나 최소화되어야 한다.

전해연마시 전해액으로는 H3PO4 420ml, glycerin 470ml, 이차증류수 150ml의 혼합 용액을 사용하였고, 교정용선재는 0.017″×0.025″굵기의 stainless steel선재와 Elgiloy선재를 사용하였으며, 249A/d□, 332A/d□, 20℃, 25℃의 조건을 달리하여 시간별로 전해연마를 시행한후 교정용선재의 폭, 단면형태 그리고 표면상태의 변화를 관찰하여 다음과 같은 결론을 얻었다.

1. 249A/d□와 20℃, 249A/d□와 25℃, 332A/d□와 20℃, 332A/d□와 25℃의 각 조건에서 stainless steel선재와 Elgiloy선재를 전해연마후 연마시간의 경과에 따라 변화된 선재폭(wire width)의 크기에 대한 평균치와 표준편차를 구하였다.

2. 전해연마 시간의 경과에 따라 stainless steel선재와 Elgiloy선재의 폭은 거의 정비례적으로 감소하였다.

3. 전해액 온도가 20℃인 실험군과 25℃인 실험군 사이에서는 연마양이 유의한 차이를 나타내지 않았으나, 전류양이 249A/d□인 실험군과 332A/d□인 실험군 사이에서는 유의한 차이를 나타내었다.

4. 전해연마후 stainless steel선재의 단면은 거의 형태변화가 없었으나, Elgiloy선재의 단면에는 모서리 부근이 더욱 동그러진 형태변화가 관찰되었다.

5. 전해연마후 선재의 표면은 stainless steel선재와 Elgiloy선재에서 모두 연마전에 비해 더욱 매끄러운 상태를 보였다.

An Experimental Study on Changes of Orthodontic Wires After Electropolishing

Jai-Chul Lee

Faculty of Dental science, Chonnam National University

Graduate School

(Directed by associated professor Jong-Chul Kim)

(Abstract)

Guiding a tooth along an arch wire results in a counteracting frictional force among arch wires, bracket and ligature. This frictional forces should be eliminated or minimized when orthodontic tooth movement is being planned.

The purpose of this study was to evaluate the changes of width, cross-sectional forms an surface morphologies of stainless steel wire and Elgiloy□ wire after electropolising. Experimental variables included in this experiment were arch wire materials, current, electrlyte temperature and polishing time. Wire widths were measured by micrometer and crass-sectional forms and surface morphologies were examined with optical microscope and scanning electron microscope

The results were as follows :

1. The mean and standard deviation of widths of stainless steel wire and Elgiloy□ wire    varying polishing time with condition of 249A/dm2 aud 20℃, 249A/dm2 and 25℃,        332A/dm2 and 20℃ and 332A/dm2 and 25℃ were obtained.

2. With increasing polishing time, the widths of stainless steel wire and Elgiloy□ wire    became decreased proportionally .

3. The changes of widths of stainless steel wire and Elgiloy□ wire were statistically      insignificant between 20℃ group and 25℃ group, but significant between 249A/dm2      group and 332A/dm2 group.

4. The cross-sectional forms of wire after electropolishing were not changed in stainless    steel wire, and while it were changed to rounded corners in Elgiloy□ wire.

5. The surface morphologies of wire after electropolishing were scratch-absent and more    smoothened both in stainless steel wire and Elgiloy□ wire.