간접부착술식시 치면과 레진 베이스의 간격 및

접착제에 따른 결합강도

서   미   영

전남대학교 대학원 치의학과

(지도교수 : 박병주)

(초록)

본 연구는 브라켓 간접부착술식시 치면과 레진 베이스의 간격 및 접착제에 따른 전단결합강도를 비교함으로써 브라켓 간접부착의 접착제로서 호제(paste)형 레진 병용의 타당성 여부를  평가해보고자 시행되었다.

소의 하악 중절치 120개를 실험재료로 하여 대조군의 경우 접착제로 실런트만을 사용하는 반면 실험군의 경우 실런트와 호제형 레진을 병용하여, 치면과 레진 베이스 간의 간격이 0.0, 0.2, 또는 0.4 mm가 되도록 접착한 다음 만능물성 시험기를 이용하여 각 시편의 전단결합강도를 측정하고 비교하여 다음의 결과를 얻었다.

1. 치면과 레진 베이스 간의 간격이 멀어질수록 두 군 모두에서 전단결합강도가 감소하는 것으로 나타났다.

2. 치면과 레진 베이스 간의 간격이 0.0 mm인 경우 양 군 간의 전단결합강도의 차이는 나타나지 않았다.

3. 치면과 레진 베이스 간의 간격이 0.2, 0.4 mm인 경우 실런트와 함께 호제형 레 진을 병용한 경우의 전단결합강도가 실런트만 사용한 경우에 비하여 통계적으로 유의하게 높게 나타났다.

이상의 연구결과는 브라켓 간접부착술식시 치면과 레진 베이스 간의 간격이 의심될 경우 브라켓 간접부착의 접착제로서 실런트만 단독 사용하는 것보다 호제형 레진을 병용하는 것이 유리함을 시사하였다.

Bond Strength According to the Adhesive Type

and the Distance Between Enamel Surface

and Resin Base in Indirect Bonding

Mi-Young Seo

Faculty of Dental Science

Graduate School, Chonnam National University, Kwangju, Korea

( Directed by Associate Professor Byung-Ju Park )

( Abstract )

The purpose of this study was to evaluate the feasibility of the combined use of paste resin with sealant as an adhesive of the indirect bonding. The resin bases made of light-cured resin were bonded to the bovine incisors at a distance of 0.0, 0.2 or 0.4 mm using the sealant only or the mixture of sealant and paste resin. Bond strength of each group was measured using universal testing machine.

The results were as follows:

1. The bond strength was reduced in both groups as the distance between          enamel surface and resin base increased.

2. The bond strength showed no statistical difference between two groups in case the distance between enamel surface and resin base was 0.0 mm.

3. In case the distance between enamel surface and resin base was 0.2 or 0.4mm, the sealant with paste resin group showed significantly higher bond strength than the sealant only group.

The results of the present study indicate that the use of paste resin with sealant may be desirable as an adhesive in indirect bonding, particularly in case a gap is suspected between enamel surface and resin base.