PLASTIC BRACKET과 METAL BRACKET상에서

수종 교정선의 마찰력에 관한 연구

조  명  숙

전남대학교 대학원 치의학과

(지도교수 : 김종철)

(초록)

고정성 교정장치를 이용한 치아이동시 tube, bracket, elastic 및 교정선간에 발생되는 마찰력은 치아이동을 저해하는 요인으로 작용할 수 있으며, 마찰력은 접촉면적, 접촉면에서 작용하는 힘, 접촉면의 형태 등 여러 요소들에 의해서 변화될 수 있다.

본 연구에서는 건조 환경하에서 bracket의 종류(plastic bracket, metal bracket), 교정선의 종류(stainless steel, Elgiloy, TMA) 및 직경( .016 inch, .018 inch)에 따른 마찰력과 2.5mm 이동할 때까지의 에너지를 측정하여 다음과 같은 결과를 얻었다.

1. plastic bracket이 metal bracket보다 더 큰 마찰력을 보였다.

2. .018 inch 교정선이 .016 inch 교정선보다 더 큰 마찰력을 보였다.

3. 교정선의 종류에 따른 마찰력의 크기는 stainless steel, Elgiloy 그리고 TMA 순으로 크게 나타났다.

4. 교정선의 종류에 다른 마찰력의 차이는 metal bracket에서 더 크게 나타났으며, 교정선의 직경에 따른 마찰력의 차이는 plastic bracket에서 더 크게 나타났다.

5. metal bracket상의 .016 inch stainless steel 교정선이 가장 작은 마찰력을 나타내었다.

Frictional Forces of various orthodontic wires

on the plastic and metal brackets

Myeong-Sook Cho

Faculty of Dental science, Chonnam National University

Graduate School

(Directed by associated professor Sung-Su Chung)

(Abstract)

Frictional forces occured between tube, bracket or elastics and archwires by fixed orthodontic appliance prevent from tooth movement, and can be changed by several factors as the area of the contact surface nomal forces, and the form of the contact surface.

This study was about frictional forces from the species of the bracket(metal bracket, plastic bracket), the species of the wire(stainless steel, Elgiloy, TMA)and the diameter of the wire(.016 inch, .018 inch), and energy produced by movement of the wire on the bracket to 2.5mm under the dry condition.

The results were as follows :

1. Frictional force from the plasic bracket was larger than that from the metal bracket.

2. Frictional force from the  .018 inch wire was larger than that from the .016 inch wire.

3. Frictional force from the species of the orthodontic wire was increased in turn

as stainless  steel,  Elgiloy and TMA.

4. The dimensional difference of frictional force occured from the species of the  orthodontic

wire was larger at metal bracket than at plastic bracket, and the dimensional difference of          frictional force occured from the diameter was larger at  plastic bracket than at metal bracket.

5. The least frctional force was seen in the .016 inch stainless steel  wire on th metal                bracket.