침수 및 온도변화에 따른

레진 브라켓 ［ing의 파절강도 비교

손   지   형

전남대학교 대학원 치의학과

(지도교수 : 황현식)

(초록)

본 연구는 침수 및 온도변화에 따른 레진 브라켓 wing의 파절양상을 비교하여 구강내 환경이 레진 브라켓 wing의 물성변화에 미치는 영향을 관찰해 보기 위하여 시행되었다.

본 연구의 재료로 레진 브라켓 75개와 금속 브라켓 25개를 사용하였는데, 레진 브라켓은 상온에서 6개월 동안 방치한 경우와 37℃의 증류수에 6개월 동안 침수시킨 경우, 그리고 37℃의 증류수에 6개월 동안 침수시킨 상태에서 1개월에 350회씩 총 2,100회의 열변환 시킨 경우의 3가지 군으로 구분하여 처리하였다. 만능물성 시험기를 이용하여 금속 브라켓의 경우 wing의 변형강도를, 레진 브라켓의 경우 파절강도를 각 군별로 측정하고 비교 분석하여 다음과 같은 결과를 얻었다.

1. 금속 브라켓 wing의 변형강도에 비하여 레진 브라켓 wing의 파절강도가 매우 낮게 나타났으며 통계적으로 유의한 차이가 있었다(p<0.001).

2. 상온에서 6개월 동안 방치한 군에 비하여 침수시키거나 침수 및 열변환 시킨 군에서 브라켓 wing의 파절강도가 낮게 나타났으며 통계적으로 유의한 차이를 보였다(p<0.001).

3. 단순침수에 비하여 침수 및 열변환 시킨 군의 브라켓 wing의 파절강도가 더 낮게 나타났으며 통계적으로 유의한 차이가 있었다(p<0.001).

이상의 결과는 구강내 환경에 의하여 레진 브라켓 wing의 물성이 약화되고 이의강도증가를 위한 대책이 필요함을 시사하였다.

Change of fracture mode of orthodontic resin bracket wings under water immersion and thermal change

Ji-Hyeong Son

Faculty of Dental Science

Graduate School, Chonnam National University, Kwangju, Korea

( Directed by Associate Professor Hyeon-Shik Hwang )

( Abstract )

The purpose of this study was to evaluate the effect of oral environment on the strength of resin bracket wings by comparing fracture mode according to water immersion and thermal change.

Seventy-five resin brackets(Spirit MB, Ormco, California) were divided into three groups and treated for six months as follows; (1) untreated, (2) water immersion in distilled water at 37℃, (3) water immersion in distilled water at 37℃ with total 2,100 times of thermocycling taken 350 times each month. Fracture mode of the wing was tested on universal testing machine. In addition to resin brackets, 25 metal brackets were used as controls. Through the statistical analyses, following results were obtained.

1. Resin bracket wings showed significantly lower fracture strength than metal             brackets(p<0.001).

2. Water immersion and water immersion with thermocycling groups showed               significantly lower fracture strength than open air condition group(p<0.001).

3. Water immersion with thermocycling group showed significantly lower                   fracture strength than water immersion group(p<0.001).

The above results suggest that the mechanical property of resin bracket wing may be influenced by oral environment and further research is needed to improve the strength of the wing in the resin bracket.